CENTURION REFRACTORIES(pTY) LTD

23 SCHÖNLAND DRIVE, FERROBANK,WITBANK,IO35

( 013 – 699 0749,  061 468 5094 cenref@mweb.co.za

PRODUCT DATA

	PRODUCT NAME
	CENTURAM M90C

	

	CHEMICAL ANALYSIS

SiO2



%

Al2O3



%

Fe2O3



%

CaO + MgO


%

C                                                     %
	  1.0
  0.3
    0.28
 90.6 

7 
	

	PHYSICAL PROPERTIES 

Bulk Density Dried @ 110 C

g/cm3
Cold Crushing Strength Dried @ 110 C
Mpa

Cold Crushing Strength Fired to 1000 C
Mpa

Maximum Particle Size


mm

Maximum Service Temperature

C

Permanent Linear change fired to 1000 C
%

Thermal Conductivity @ 1000 C

W/mK

ADDITIONAL INFORMATION 

Water Addition



%

Shelf-Life




months

Packaging Size                                
kg

DESCRIPTION 

APPLICATION 


	2.6
30
50
  5
                                            1850

  -0.10 

 2.7
 –

3
25 
Dead burned magnesite based ramming material with carbon addition.                                            

Extreme temperature conditions.
	


THIS DATA IS BASED ON AVERAGE VALUES AND SHOULD NOT BE TAKEN AS A GUARANTEED SPECIFICATION.  IT IS SUBJECT TO REASONABLE VARIATION.  WHERE A PROPERTY IS CRITICAL, CONFIRMATION SHOULD BE OBTAINED FROM CENTURION REFRACTORIES..

