CENTURION REFRACTORIES(pTY) LTD

23 SCHÖNLAND DRIVE, FERROBANK,WITBANK,IO35

( 013 – 699 0749,  061 468 5094 cenman@iafrica.com

PRODUCT DATA

	PRODUCT NAME
	
CENTURMOR  M90

	

	CHEMICAL ANALYSIS 

SiO2




%

Al2O3




%

Fe2O3




%

TiO2




%

CaO + MgO



%

K2O + Na2O



%

Cr2O3




%

P2O5




%
	
2

91

1.4


1.5


1.2


2.0


-


-
	

	PHYSICAL PROPERTIES 

Bulk Density Dried @ 110 C

g/cm3
Cold Crushing Strength Dried @ 110 C
Mpa

Cold Crushing Strength Fired to 1000 C
Mpa

Maximum Particle Size


mm

Maximum Service Temperature

C

Permanent Linear change fired to 1000 C
%

Thermal Expansion at 1000 C

%

Thermal Conductivity @ 1000 C

W/mK

ADDITIONAL INFORMATION 

Water Addition



%

Shelf Life




months

Packaging Size                                       
kg

No. bags per pallet

Mass required per 1 000 Bricks                  kg

DESCRIPTION 

APPLICATION

	
-


-


-


0.5


1800


-


-


-


30

6


20


60


225


AIR SETTING DRY MORTAR


For use with basic bricks (MgO, MgO/Carbon and    Chromag)

	


THIS DATA IS BASED ON AVERAGE VALUES AND SHOULD NOT BE TAKEN AS A GUARANTEED SPECIFICATION.  IT IS SUBJECT TO REASONABLE VARIATION.  WHERE A PROPERTY IS CRITICAL, CONFIRMATION SHOULD BE OBTAINED FROM CENTURION REFRACTORIES.

